774
ARCHITECTURAL AND INDUSTRIAL MAINTENANCE COATING – STANDARDS
774.1
No person shall manufacture, blend, supply, sell, offer for sale, apply, or solicit the application of any architectural coating with a VOC con​tent in excess of the corresponding limit specified in the Table of Standards in § 774.10, except as provided in §§ 774.2, 774.3, 774.8, and 774.10.  

774.2 
The most restrictive VOC content limit shall apply if anywhere on the container of any architectural coating, or any label or sticker affixed to the container, or in any sales, advertising, or technical liter​ature supplied by a manufacturer or anyone acting on their behalf, any representation is made that indicates that the coating meets the definition of or is recommended for use for more than one (1) of the coating categories listed in the Table of Standards in § 774.10. This pro​vision does not apply to the following coating categories:

(a) Lacquer coatings (including lacquer sanding sealers);

(b)
Metallic pigmented coatings;

(c)
Shellacs;

(d)
Fire‑retardant coatings;

(e)
Pretreatment wash primers;

(f)
Industrial maintenance coatings;

(g)
Low‑solids coatings;

(h)
Wood preservatives;

(i)
High‑temperature coatings;

(j)
Temperature‑indicator safety coatings;

(k)
Antenna coatings;

(l)
Antifouling coatings;

(m)
Flow coatings;

(n)
Bituminous roof primers;

(o)
Specialty primers, sealers, and undercoaters;

(p)
Thermoplastic rubber coating and mastic;

(q)
Calcimine recoaters;

(r)
Impacted immersion coatings;

(s)
Nuclear coatings; and

(t)
Concrete surface retarders.

774.3
A coating manufactured before the effective date specified for that coating in the Table of Standards in § 774.10, may be sold, supplied, or offered for sale after the specified effective date. In addition, a coating manufac​tured before the effective date specified for that coating in the Table of Standards in § 774.10 may be applied at any time, both before and after the specified effective date, so long as the coating complied with the standards in effect at the time the coating was man​ufactured. This subsection does not apply to any coating that does not display the date or date code required by § 776.1(a).

774.4
All architectural coating containers used to apply the contents therein to a surface directly from the con​tainer by pouring, siphoning, brushing, rolling, padding, ragging, or other means shall be closed when not in use. These architectural coatings containers include, but are not limited to:

(a) 
Drums, buckets, cans, pails, trays, or other application containers; and 

(b)
Containers of any VOC‑containing materials used for thinning and cleanup shall also be closed when not in use.

774.5
No person who applies or solicits the application of any architectural coating shall apply a coating that is thinned to exceed the applicable VOC limit specified in the Table of Standards in § 774.10.

774.6
No person shall apply or solicit the application of any rust pre​ventive coating for industrial use, unless such a rust preven​tive coating complies with the industrial maintenance coating VOC limit specified in the Table of Standards in § 774.10.

774.7
For any coating that does not meet any of the definitions for the specialty coatings cate​gories listed in the Table of Standards in § 774.10, the VOC content limit shall be deter​mined by classifying the coating as a flat coating or a non‑flat coating, based on its gloss, as defined in § 799, and the corresponding flat or non‑flat coating limit shall apply.

774.8
A manufacturer, seller, or user of an industrial maintenance coating may petition the Department to apply an industrial maintenance coating with a VOC content greater than three hundred forty gallons per liter (340 g./L) if all of the following conditions are met:

(a)
The industrial maintenance coating is applied outside the ozone season, normally May through September every year;

(b)
The petition submitted to the Department shall contain the following information, as applicable: job requirements and descriptions, volume of coating, maximum VOC content, and a cer​tification that a complying coating meet​ing the job performance requirements is not available; and

(c)
If the Department grants written approval, such approval shall contain volume and VOC limit conditions. Until written approval is granted by the Department and received by the petitioner, all provisions of this section shall apply.

774.9
The Department shall not approve any petition under § 774.8 if the approvals previously granted by the Department during the calendar year, when combined with the petition under consideration, would result in excess VOC emissions for that calendar year that would exceed five percent (5%) of the annual emission reduction achieved within the District of Columbia from implementing the January 1, 2005, VOC limit for industrial maintenance coatings. Coatings subject to this provision shall be sold only if an approved petition (or a copy of it) is provided before the sale. Coatings subject to this provision shall not be available to the general public.

774.10
Notwithstanding the provisions of § 774.1, a person or facility may add up to ten percent (10%) by volume of VOC to a lacquer to avoid blushing of the finish during days with relative humidity greater than seventy percent (70%) and tem​perature below sixty-five degrees Fahrenheit (65° F) or eighteen degrees Celsius (18º C) at the time of application, provided that the coating contains acetone and no more than five hundred fifty grams (550 g.) of VOC per liter of coating, less water and exempt compounds, before the addition of VOC.
Table of Standards. VOC Content Limits for Architectural Coatings.
 
	Coating Category


	VOC Content Limit

(Grams VOC per liter)


	Flat coatings
	100

	Non‑flat coatings
	150

	Non‑flat high gloss coatings
	250

	Specialty Coatings
	

	Antenna coatings
	530

	Antifouling coatings
	400

	Bituminous roof coatings
	300

	Bituminous roof primers
	350

	Bond breakers
	350

	Calcimine recoater
	475

	Clear wood coatings:
	

	• Clear brushing lacquers
	680

	• Lacquers (including lacquer sanding sealers)
	550

	• Sanding sealers (other than lacquer sanding sealers)

	350

	• Varnishes
	350

	Concrete curing compounds
	350

	Concrete surface retarders
	780

	Conjugated oil varnish
	450

	Conversion varnish
	725

	Dry fog coatings
	400

	Faux finishing coatings
	350

	Fire‑resistive coatings
	350

	Fire‑retardant coatings
	

	• Clear
	650

	• Opaque
	350

	Floor coatings
	250

	Flow coatings
	420

	Form‑release compounds
	250

	Graphic arts coatings (sign paints)
	500

	High‑temperature coatings
	420

	Industrial maintenance coatings
	340

	Impacted immersion coatings
	780

	Low‑solids coatings

	120

	Magnesite cement coatings
	450

	Mastic texture coatings
	300

	Metallic pigmented coatings
	500

	Multi‑color coatings
	250

	Nuclear coatings
	450

	Pre‑treatment wash primers
	420

	Primers, sealers, and undercoaters
	200

	Reactive penetrating carbonate stone sealer
	600

	Quick‑dry enamels
	250

	Quick‑dry primers, sealers and undercoaters
	200

	Recycled coatings
	250

	Roof coatings
	250

	Rust preventative coatings
	400

	Shellacs
	

	• Clear
	730

	• Opaque
	550

	Specialty primers, sealers, and undercoaters
	350

	Stains
	250

	Stone consolidants
	450

	Swimming pool coatings
	340

	Swimming pool repair and maintenance coatings


	340

	Temperature‑indicator safety coatings
	550

	Thermoplastic rubber coatings and mastics
	550

	Traffic marking coatings
	150

	Waterproofing sealers
	250

	Waterproofing concrete/masonry sealers
	400

	Wood preservatives
	350



SOURCE: Notice of Final Rulemaking published at 58 DCR 11286, 11397 (December 30, 2011).

� Limits are expressed in grams of VOC per liter of coating thinned to the manufacturer's maximum recommendation, excluding the volume of any water, exempt compounds, or colorant added to tint bases.  Manufacturer’s maximum recommendation means the maximum recommendation for thinning that is indicated on the label or lid of the coating container.  





� Conversion factor: one pound VOC per gallon (U.S.) is equivalent to one hundred nineteen and ninety-five one hundredths grams per liter (119.95 g/L).


� Units for this coating are grams of VOC per liter (pounds of VOC/gallon) of coating, including water and exempt compounds








